HAYES PARK CENTRAL AND SOUTH BLOCKS

Method statement for removal of smooth render applied to colums at lower levels at the above locus.

1 – Remove existing render by means of sand blasting until exposed aggregate finish starts to appear.
2 – Brush down to remove any loose material.
3 – Working one face at a time thoroughly soak the face of the colum to reduce suction.
4 – Apply a hydrochloric acid based masonry cleaner, 5% concentration and agitate with stiff bristle brush and leave to activate but not dry out.
5 – Flood surface working top to bottom to remove residue and assess finish.
6 – Repeat item 5 until desired finish is required.




