Method Statement

Fireplace Exploratory Work : 25a The Green, UB7 7PN

- All the rebuilding/restoration work is carried out by hand, using reclaimed period bricks, stone, brick paviours for the hearth, oak timbers. Materials used for the restorations/repairs around the country varied in there type and colour according to the local supply and varied in size according to the period in history in which they were constructed. Materials will be used such as bricks, stones which are reclaimed and are the correct type, colour and size for each individual fireplace. All mortar will be removed when loose by hand and the rest removed with suitable plugging chisel again by hand. All broken and deteriorated bricks will be cut out, clean and replace like for like again by hand and then repointing of the inglenook fireplace will be done by hand using lime mortar.

- To remove the modern plaster and the cement render. To cut out any modern or deteriorated brickwork/ stonework and rebuild as necessary to original format. Restore remainder of brickwork/stonework. If any original alcoves are found during the restoration /repair work - they will be rebuild / repaired to the original format then lime plaster and lime wash the internal back walls. Once the hearth is exposed to check for remains of the original one and  if a modern one is to be found - to take out and relay a brick hearth flush with the two brick pillars.

- For all lime based materials like NHL 3.5, lime mortar and lime plaster the company based in Reading - Old House Store Store will be used as a supplier.

- The proposed works are to be carried out to the above Listed two story building and would not affect any of the features for which it was listed. The proposed work would restore the inglenook fireplace to its original appearance. The inglenook fireplace is approximately .....wide,......high and .....deep and it is now completely block by a modern infill. To preserve that important part of the building a specialist inglenook company with more than 15 years experience in working on old historic buildings will be the contractor for the project - Inglenook Restoration LTD. The restoration/repair work will be constructed using external materials to match those on the existing building in colour, texture, form and composition.  As well as the restoration work, there is the opportunity to remedy the damp problem in the area. The proposed work would not further develop any of the existing site, or increase any accommodation, nor alter any relationship of the site to the rest of the building, internally or externally.

Deyan Kovachev

Inglenook Restoration Ltd

References: