Technical Specifications for Daltex performance uvr resin

The full Technical Specifications for DALTEX Performance UVR Resin outline its material properties, mixing criteria, and performance parameters.

Material Properties & Composition

- Resin Type: Two-part Aliphatic Polyurethane (Solvent-free, 100% solids).

- UV Resistance: 100% UV stable; will not yellow, discolour, or become brittle under sunlight.

- Component Kit: Part A (Polyol) and Part B (Isocyanate).

- Kit Weight: 7.5 kg total.

- Mix Ratio: 1 : 1.04 by weight.

Performance & Compliance

- Certification: Fully BBA Approved (British Board of Agrément) when mixed according to specification.

- Permeability: Highly porous; allows water to drain freely at rates exceeding 850mm per hour when laid as a system.

- Tensile Strength: Engineered for high structural flexibility to resist cracking from thermal movement.

- Product Guarantee: 15-year quality assurance against material failure.

Application Parameters

- Working Temperature: Ideal installation range between 5°C and 30°C.

- Relative Humidity: Must be below 80% during application; substrate must be completely dry.

- Pot Life: Approximately 20–30 minutes at 20°C (decreases in hotter weather).

- Curing Profile: Pre-catalysed for standard seasonal temperatures; accepts foot traffic in 4–8 hours and vehicular traffic in 16–24 hours at 20°C.