Technical Specifications for Daltex performance uvr resin
The full Technical Specifications for DALTEX Performance UVR Resin outline its material properties, mixing criteria, and performance parameters.
Material Properties & Composition
· Resin Type: Two-part Aliphatic Polyurethane (Solvent-free, 100% solids).
· UV Resistance: 100% UV stable; will not yellow, discolour, or become brittle under sunlight.
· Component Kit: Part A (Polyol) and Part B (Isocyanate).
· Kit Weight: 7.5 kg total.
· Mix Ratio: 1 : 1.04 by weight.
Performance & Compliance
· Certification: Fully BBA Approved (British Board of Agrément) when mixed according to specification.
· Permeability: Highly porous; allows water to drain freely at rates exceeding 850mm per hour when laid as a system.
· Tensile Strength: Engineered for high structural flexibility to resist cracking from thermal movement.
· Product Guarantee: 15-year quality assurance against material failure.
Application Parameters
· Working Temperature: Ideal installation range between 5°C and 30°C.
· Relative Humidity: Must be below 80% during application; substrate must be completely dry.
· Pot Life: Approximately 20–30 minutes at 20°C (decreases in hotter weather).
· Curing Profile: Pre-catalysed for standard seasonal temperatures; accepts foot traffic in 4–8 hours and vehicular traffic in 16–24 hours at 20°C.


